## Slide 1
Notes: UV-visible absorption (black) and emission (red) profiles of dyes IrD and JM, recorded from micromolar acetonitrile solutions.
1

## Slide 2
Notes: Emission spectra of 1%IrD, 1%JM and 1%IrD-1%JM, recorded from 0.3 mg/mL cyclohexane suspensions, at an excitation wavelength of 300 nm and 3 nm bandwidth.

## Slide 3
Notes: Decay profiles of 1%IrD and 1%IrD-1%JM, recorded at an emission wavelength of 463 nm, using a 375 nm laser source

## Slide 4
Notes: Emission spectra of 5%IrD, 5%JM and 5%IrD-5%JM, recorded from 0.3 mg/mL cyclohexane suspensions, at an excitation wavelength of 300 nm and 5 nm bandwidth.

## Slide 5
Notes: Decay profiles of 5%IrD and 5%IrD-5%JM, recorded at an emission wavelength of 463 nm, using a 375 nm laser source