This is the simple example template containing only headers for each report item and the bookmarks. The invisible bookmarks are indicated by text between brackets.

Modify it according to your own needs and standards.

## Measurement Conditions:  (Bookmark 1)

Dataset Name	MW-1

File name	H:\Downloads\MW-1.xrdml

Sample Identification	MW-1

Comment	Configuration=Sample changer, Owner=User-1, Creation date=29/10/2008 13:01:45

Goniometer=PW3050/60 (Theta/Theta); Minimum step size 2Theta:0.001; Minimum step size Omega:0.001

Sample stage=Spinner PW3064

Diffractometer system=XPERT-PRO

Measurement program=C:\PANalytical\Data Collector\Programs\Main scan with monochromator.xrdmp, Identifier={5C688D29-6B23-498B-9D06-B762B64CDECE}

Batch program=C:\PANalytical\Data Collector\Programs\Batch-3.xrdmp, Identifier={5D80FBE9-2F3F-447F-B8D2-149A342178AF}

Monochromator fitted to the diffracted optics

## Main Graphics, Analyze View: (Bookmark 2)

## Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 18.5496 | 173.26 | 0.3897 | 4.77944 | 2.48 |
| 30.3979 | 1759.02 | 0.2273 | 2.93815 | 25.13 |
| 35.7525 | 6999.81 | 0.2598 | 2.50943 | 100.00 |
| 37.3982 | 396.61 | 0.2598 | 2.40269 | 5.67 |
| 43.3722 | 1841.76 | 0.3247 | 2.08458 | 26.31 |
| 53.7692 | 933.97 | 0.2598 | 1.70347 | 13.34 |
| 57.2377 | 2913.59 | 0.2598 | 1.60820 | 41.62 |
| 62.9173 | 4724.75 | 0.2922 | 1.47600 | 67.50 |
| 71.3594 | 401.61 | 0.3897 | 1.32069 | 5.74 |
| 74.3957 | 994.06 | 0.2598 | 1.27413 | 14.20 |
| 75.4029 | 356.29 | 0.3247 | 1.25959 | 5.09 |
| 79.2618 | 261.16 | 0.3247 | 1.20767 | 3.73 |
| 82.6372 | 113.73 | 0.7793 | 1.16669 | 1.62 |
| 87.0336 | 419.81 | 0.3247 | 1.11870 | 6.00 |
| 89.8989 | 1351.42 | 0.5845 | 1.09033 | 19.31 |
| 94.7160 | 543.94 | 0.3897 | 1.04717 | 7.77 |